## Slide 1: Fatigue Test Modeling For The European INCEFA-SCALE Project
Author: Raphael ALVES HAILER
ENSTA Paris tutor: Anne-Lise GLOANEC
Host organization tutor: Stéphan COURTIN

## Slide 2
1
Introduction and contextualization
2
Theoretical foundations of fatigue assessment
3
The Chaboche Constitutive Model
4
Multi-objective optimization and evolutionary algorithms
5
Results and discussion
6
Conclusion
2/62

## Slide 3
1
Introduction and contextualization
3/62

## Slide 4: The nuclear industry
The nuclear sector is crucial in the global energy landscape
  As of 2021, 69% of France’s total generation comes from nuclear plants
  Considered a clean energy source
Problem of aging
  Average nuclear reactor age worldwide: 31.9 years
  In Europe, the average is of 35.6 years
Susceptibility to failure due to Fatigue
4/62

## Slide 5: INCEFA-SCALE project
Counts with multiple academical and industrial partners
  Framatome, CEA, Kaunas University of Technology (KTU), …
Works on Environmentally Assisted Fatigue (EAF)
Objectives:
  Fill the laboratory-to-scale knowledge gap
  Improve the lifetime predictions of components in a Nuclear Power Plant (NPP)
  Review international guidelines to enhance the reliability of NPP components, such as the NUREG/CR-6909 Revision 1 report, from the United States Nuclear Regulatory Comission (NRC)
5/62

## Slide 6: Computational tools used
Numerical simulations conducted using Salome Meca
  Combination of Salome and code_aster
  Open source software developed by EDF
  Possible to integrate Python, C++, C or Fortran code.
Salome:
  Powerful tool for CAD modeling, meshing, pre-processing and post-processing
code_aster
  Finite elements solver with easy to implement syntax
  Possible to study a broad range of physical phenomena
6/62

## Slide 7: Objective of this work
Conduct numerical simulations so as to:
  Reproduce the experiments from INCEFA-SCALE partners on the SAE 316L stainless steel
  Validate the use of code_aster to accurately describe the mechanical behavior of laboratory specimens
  Compare Finite Elements Analysis (FEA) results with test results
Additionally, experiment with different Chaboche constitutive model parameter sets
7/62

## Slide 8
2
Theoretical foundations of fatigue assessment
8/62

## Slide 9: Motivation
Industrialization
  Economy heavily based on mass production, driven by mechanized manufacturing
  Machines and transports depending on axles and rotating pieces
  Components subjected constantly to cyclic loads
Catastrophic failures
  Often lethal, caused by the fatigue phenomenon
  Affects different sectors, such as aeronautical, mining and railway
9/62

## Slide 10: Motivation
Lithograph of the Versailles-Paris railway accident in may 8, 1842. Courtesy of the Bibliothèque Nationale de France
10/62
Failure due to cyclic pressurization in the de Havilland Comet I aircraft, the first commercial jet airliner, in 1954. Courtesy of the Royal Air Force (RAF) museum

## Slide 11: Fatigue
Phenomenon where cyclic loads with lead to rupture of a material
  Surface imperfections
  Stress concentration K
  Vacancies
Cumulative damage promotes crack growth throughout material’s lifetime
Paris law used to predict the rate of fatigue frack growth
11/62

## Slide 12: Crack Growth
12/62
Ahmadivala, Morteza: Towards optimal maintenance planning of existing structures based on time-dependent reliability analysis. PhD thesis, December 2020.
Ghodrat, Sepideh, Ton Riemslag, and Leo AI Kestens: Measuring plasticity with orientation contrast microscopy in aluminium 6061-t4. Metals, 7(4):108, 2017.

## Slide 13: Fatigue life stages
Two fatigue life stages of interest for the INCEFA-SCALE project:
  Maximum hardening stage
    Early fatigue life
    Material experiences cyclic hardening
  Half life stage
    Life stage where the number of cycles is half the necessary for rupture
    Most real life machinery components are in this stage. Hence the importance of characterizing it accurately
    Corresponding to stabilized cyclic behavior
13/62

## Slide 14
3
The Chaboche Constitutive Model
14/62

## Slide 15: Chaboche constitutive model
All numerical simulations considered the Chaboche constitutive model
  Designed as a way to characterize the 316L stainless steel
  Mathematical model with equations that account for the kinematic and the isotropic hardening effects
  Particular focus on cyclic plasticity
  Accounts for strain accumulation and recovering
15/62

## Slide 16: Chaboche constitutive model
16/62
code_aster is able to implement it easily
  With history effect
    Variable amplitude loading
  Without history effect
In the present work, we consider 2 kinematic hardenings
One approach on parameter identification can be to solve an optimization problem

## Slide 17: Chaboche constitutive model
Important mechanical quantities
  In the whole study, we are going to rely in measures of two important mechanical quantities:
    Von Mises equivalent stress
    Von Mises equivalent strain
17/62

## Slide 18
4
Multi-objective optimization and evolutionary algorithms
18/62

## Slide 19: Basics of multi-objective optimization
19/62
Optimization problems where two or more objectives are considered
Objective: determine the Pareto front
  Set of designs that dominates all others
Typical mathematical formulation without constraints:

## Slide 20: Evolutionary algorithms
Based on principles of natural selection
  Survival of the fittest
Genetic information DoE parameters
Uses of crossover and mutation operators
In this study, the NSGA-II algorithm is used
  Crossover operator: Simulated Binary Crossover (SBX)
  Mutation Operator: Polynomial Mutation
  Individuals ranked according to their ranks and crowding distances
20/62

## Slide 21: NSGA-II workflow and pseudocode
21/62
Deb, K., A. Pratap, S. Agarwal, and T. Meyarivan: A fast and elitist multiobjective genetic algorithm: Nsga-ii. IEEE Transactions on Evolutionary Computation, 6(2):182–197, 2002

## Slide 22
Results and discussion
5
22/62
Part 1 – Validation of code_aster modeling
Part 2 - Testing Chaboche parameter sets
Part 3 – Optimization of parameters
Part 4 – OPT parameters on specimens
Part 5 – Variable amplitude loading

## Slide 23: Notched specimen
Study on the effects of geometry and load on notched specimens
3 geometrical parameters:
  Nominal Diameter
  Reduced diameter
  Notch radius
Interest behind notched specimens:
  Stress concentration region
  Susceptible to crack generation
  Common practice among experimental campaigns on fatigue
All simulations considered T = 300°C
23/62

## Slide 24: Part 1 – Validation of code_aster modeling
Meshes used
  Symmetry boundary conditions applied in order to use smaller domain and refine the mesh
Red dot
  Extensometer measurement
24/62
Notch root

## Slide 25: Part 1 – Validation of code_aster modeling
Initial validation of code_aster framework using cyclic stress-strain curves on INCEFA-SCALE diagnostic tests
Monotonic stress loading
25/62

## Slide 26: Part 1 – Validation of code_aster modeling
Comparison of used curves with available experimental data at maximum hardening and half life stages of fatigue life
26/62

## Slide 27: Part 1 – Validation of code_aster modeling
Results (Notch, Extensometer)
27/62
Errors similar to FRF (reference)
Reference

## Slide 28: Part 1 – Validation of code_aster modeling
Present code_aster modeling is considered to have been well implemented
This gives credibility to further simulation results
28/62

## Slide 29: Part 1 – Validation of code_aster modeling
General strain and stress profiles (FRF specimen)
29/62

## Slide 30: Part 2 – Testing Chaboche parameter sets
30/62
Former strategy cannot be used for cyclic simulations
Objective: test the parameter sets provided by CEA in the INCEFA-SCALE project and Zhang’s parameter set*
We seek to determine if any of these parameter sets is good enough to proceed with full-scale specimen simulations
First approach:
  Used simple cubic mesh to reduce computational burden
*Zhang, Wen: Fatigue crack growth in large scale yielding condition. PhD thesis, Université Paris Saclay (COmUE), 2016.

## Slide 31: Part 2 – Testing Chaboche parameter sets
31/62
Mesh and boundary conditions:
  Nodes 1, 2, 3 and 4: no displacement in the z direction
  Nodes 1, 2, 5 and 6: no displacement in the y direction
  Nodes 1, 4, 5 and 8: no displacement in the x direction
  Nodes 5, 6, 7 and 8: imposed displacement in the z direction
Strain controlled simulations
  Total of 100 cycles per strain amplitude

## Slide 32: Part 2 – Testing Chaboche parameter sets
32/62
Parameter sets tested
With history effect

## Slide 33: Part 2 – Testing Chaboche parameter sets
33/62
Comparison of Zhang parameters (history effect)
Best sets:
  Maximum hardening:
    with history effect

## Slide 34: Part 2 – Testing Chaboche parameter sets
34/62
Comparison of Zhang parameters (history effect)
Best sets:
  Maximum hardening:
    with history effect
  Half life:
    without history effect

## Slide 35: Part 2 – Testing Chaboche parameter sets
Comparison with CEA parameter sets (Parameter set 1 not considered)
35/62
Conclusion:
  Maximum hardening: parameter set 3

## Slide 36: Part 2 – Testing Chaboche parameter sets
Comparison with CEA parameter sets (Parameter set 1 not considered)
36/62
Conclusion:
  Maximum hardening: parameter set 3
  Half life: parameter set 2

## Slide 37: Part 2 – Testing Chaboche parameter sets
Comparison of best parameter sets
37/62

## Slide 38: Part 2 – Testing Chaboche parameter sets
Comparison of best parameter sets
CEA sets suitable for smaller strain ranges
Zhang sets suitable for bigger strain ranges
38/62

## Slide 39: Part 2 – Testing Chaboche parameter sets
The rest of the work focuses only on analyzing the half life stage, for the interest of the INCEFA-SCALE project
The best parameter sets (Zhang without history effect and CEA 2) were tested on FRF diagnostic specimen
  Stress controlled simulation
Present FEA results are not good
   Optimization of these parameters is to be conducted
39/62

## Slide 40: Part 3 – Optimization of parameters
40/62
NSGA-II algorithm implemented considering:
  Objective functions:
  DoE:
Formulation:

## Slide 41: Part 3 – Optimization of parameters
and are fixed for all simulations
Crossover:
  increases linearly, from 2 to 20
  Probability of crossover: 0.9
Mutation
  increases linearly, from 2 to 20
  Probability of mutation: 0.1
Strain controlled simulations on cubic mesh
  Strain amplitudes considered: 0.3, 0.5 and 0.6%
  3 cycles per strain amplitude
41/62

## Slide 42: Part 3 – Optimization of parameters
Objective space for all 3 runs
  1st run:
42/62

## Slide 43: Part 3 – Optimization of parameters
Objective space for all 3 runs
  1st run:
  2nd and 3rd run:
43/62

## Slide 44: Part 3 – Optimization of parameters
Objective space for all 3 runs
  1st run:
  2nd and 3rd run:
Results tend to straight line
Recommendations:
  Increase and number of cycles
Constraints:
  Time limit of Cronos cluster
44/62

## Slide 45: Part 3 – Optimization of parameters
Obtained parameter set:
45/62

## Slide 46: Part 3 – Optimization of parameters
Hysteresis cycle comparison
46/62

## Slide 47: Part 4 –OPT parameters on specimens
1st analysis: diagnostic tests
  FRF  8 cycles / EDF  3 cycles per step / KTU  8 cycles per step
Levels of error with the same order of magnitude as those obtained by Framatome and CEA
In some cases, we get improved accuracy
47/62

## Slide 48: Part 4 –OPT parameters on specimens
Possible to obtain hysteresis cycles at notch root
48/62

## Slide 49: Part 4 –OPT parameters on specimens
Possible to obtain hysteresis cycles at notch root
49/62

## Slide 50: Part 4 –OPT parameters on specimens
Possible to obtain hysteresis cycles at notch root
and the cycle gets more asymmetrical
50/62

## Slide 51: Part 4 –OPT parameters on specimens
Implementation on specimens yet to be tested
  New meshes:
51/62

## Slide 52: Part 4 –OPT parameters on specimens
Obtained results
52/62

## Slide 53: Part 4 –OPT parameters on specimens
Conclusion:
  Zhang and CEA parameter sets were not adequate for the half life stage of the 316L steel
  Development of an optimization framework to find optimal parameter set
  Results are promising, and there is now available numerical data for experiments yet to be conducted
53/62

## Slide 54: Part 5 –Variable amplitude loading
Attempt to implement the optimized Chaboche model on Periodic Over-Underload (POUL) test
  for 2 cycles
  for 1000 cycles
Extremely important, since real life components face variable amplitudes regularly
54/62

## Slide 55: Part 5 –Variable amplitude loading
Strategy: implement Zhang parameters at and OPT parameters at
  Attempt to extract the best out of the two parameter sets
Strain controlled simulations conducted on the cubic mesh
Impossible to implement 1000 cycles atper periodic repetition
  Solution: 20 cycles to achieve stabilization, then repeat the result until 1000 cycles for comparison with experimental results
55/62

## Slide 56: Part 5 –Variable amplitude loading
56/62

## Slide 57: Part 5 –Variable amplitude loading
57/62

## Slide 58: Part 5 –Variable amplitude loading
Conclusion:
  Fairly good results for the first periodic repetition
  FEA results not capturing progressive hardening
    Zhang parameters designed to capture stress levels at maximum hardening or half life
  Furthermore, OPT parameters are not capturing previous deformation state
    Lack of history effect
  Approach of multiple constitutive model parameter sets looks promising
  Further exploration of this method could be interesting
58/62

## Slide 59
Conclusion
6
59/62

## Slide 60: Conclusion
Initially, the objective was to reproduce INCEFA-SCALE fatigue tests
Shift in research objective due to Chaboche model parameters not being suitable
Implementation of NSGA-II evolutionary algorithm to tackle this problem
Good FEA results obtained with multiple specimens
Further work must be done on variable amplitude loading tests
60/62

## Slide 61
Thank you for your attention!
61/62

## Slide 62: Main references
Zhang, Wen: Fatigue crack growth in large scale yielding condition. PhD thesis, Université Paris Saclay (COmUE), 2016.
Deb, K., A. Pratap, S. Agarwal, and T. Meyarivan: A fast and elitist multiobjective genetic algorithm: Nsga-ii. IEEE Transactions on Evolutionary Computation, 6(2):182–197, 2002
EDF: Incefa-scale report d4.2 - mo36 modelling progress. Unpublished project report, 2024.
62/62